AUTEX 2024                                                                                                            17 – 19 June 2024, Liberec

STRUCTURAL CHANGES OF UHMWPE FIBER TREATED WITH OZONE
İdil Yiğit1,2, Semiha Eren2, Zaide Saka3, Nebahat Aral Yılmaz4, Yahya Kaya5 
 1 Bursa Uludag University, Textile, Clothing, Footwear and Leather Department, Vocational School of Orhaneli, Bursa 16059, Turkey, e-mail: idilyigit@uludag.edu.tr 
2 Bursa Uludag University,Textile Engineering Department,16059, Turkey, e-mail: semihaeren@uludag.edu.tr
3 Bursa Uludag University,Textile Engineering Department,16059, Turkey, e-mail: zaidesaka@uludag.edu.tr 

4Yeditepe University, Department of Materials Science and Nanotechnology Engineering, 34755, Turkey, e-mail: nebahat.aral@yeditepe.edu.tr
5Advanced Composite Materials Technology Center, R&D and Technology Directorate, Turkish Aerospace, Ankara, Turkey, yahyaoz@metu.edu.tr 
Abstract: Since UHMWPE (Ultra-high molecular weight polyethene) has a higher molecular weight than other types of PE produced, its characteristics are much improved. It is an engineering thermoplastic with a wide range of uses [1-3]. UHMWPE is used in many different areas, such as medical, anti-ballistic and high-modulus composite and defence industries (such as clothing and rope) [4].
It is possible to increase interface bonding by creating functional groups containing active oxygen on the fiber surface through oxidation methods. The ozonation process is one of the known oxidation processes.

In this study, AFM, SEM and XPS analyzes were performed on samples that were ozonated on UHMWPE surfaces for different periods of time. Table 1 shows the roughness (Ra) data obtained from AFM. It was observed that as the ozonation time increased, there was roughness on the surface of the samples.

Figure 1 shows SEM and AFM images of the samples. 
Table 1 The AFM of ozonated UHMWPE fiber
	Process
	RMS (nm)
	Ra (nm)

	Untreated 
	530,6
	362,1

	Ozone Treated
5 l/min-60min
	545,3
	490,1

	Ozone Treated
5 l/min-120min
	767,1
	667,9


Table 2 XPS analysis results 

	   UHMWPE 

   Sample 
	Different Energy Levels C1s peaks (eV; area, %)

	
	Peak 2

284.8-
285.4 eV
	Peak 3

285.7-
286.3 eV
	Peak 4

286.6-286.7 eV
	Peak5

287.7-
288.5 eV
	Pik 6

288.8-

290.1 eV

	   Untreated 

	96.39
	0
	1.83
	0
	0

	5l/min-120min       Ozonated 
	87.26
	2.81
	2.51
	1.28
	87.26

	
	
	
	
	
	

	Bonds 
	-C-C

-C-H
	-C-OH


	-C-O-C


	-C=O

-C=N
	-COOH

-COOR


XPS analysis results; It has been observed that the ozonation process increases the hydroxyl and carbonyl groups in UHMWPE. The XPS C1s spectrum results in Table 2 show that the oxygen-containing functional groups of UHMWPE increase with the ozonation process.
	[image: image1.png]Z4is - Scan backvard_Line






	


[image: image2.png]2w - Seamtoread Lno





Figure 1 SEM and AFM images of UHMWPE  a) Untreated UHMWPE b) 5l/min 120 min ozone treated UHMWPE
Keywords: uhmwpe, surface, modification

Acknowledgement: This study is supported by Bursa Uludag University Scientific Project Department by number of FGA 2023 1258.
references

[1] Kurtz S.M., The UHMWPE handbook: ultra-high molecular weight polyethylene in total joint replacement, Elsevier, 2004.
[2] Ozcan, S., Dandan Doganci, M. The effect of polyethylene‐graft‐maleic anhydride on ultrahigh molecular weight polyethylene/carboxymethyl cellulose blends. Journal of Applied Polymer Science,2022.

